# CVD growth of Carbon nanotubes

### Substrate preparation

- Dice small squares of Si wafer , such that squares would fit inside the AFM

- Clean silicon squares by consecutive sonication in soapy water and acetone.

- Move the silicon chips from acetone to isopropanol, without letting the acetone on the surface of the chips dry. This is done by having a squeezy bottle of isopropanol ready. Pull the chip out of acetone, squirt isopropanol and drop in isopropanol solution

- Move the chip into solution of iron (III) nitrate nanohydrate in isopropanol (typically 0.0024 gm in 12 ml).

- Dip in hexane for 10 sec and then blow dry

### Growth of CNT

- Silicon squares are heating in Ar (flow rate of 0.6 l/min) to 850 degrees from room temperature

- Hydrogen in flowed in (rate of 3 ml/min) for 10 min

- Ethylene is flowed in (rate of 1 ml/min) + Hydrogen (3 ml/min) for 1 min

- Ethylene is flowed in (rate of 0.1 ml/min) + Hydrogen (3 ml/min) for 6 min

- Ar is kept flowing till the oven has reached a temperature of 200 deg or less

For programming the temperature steps of the oven , the manual is in lower drawer of the table (on which the oven sits)