Self Assembled Monolayers of alkane thiols on gold AFM tips

Recipe from Rachel McKendry, UCL

AFM Tips:

1000 Angstrom gold freshly evaporated, Balzen evaporator

Base pressure=1*10-7 mbar

Rate=1-10 Angstrom/sec

Anneal at 340 degrees C

(or use biolevers!)

Immerse in 2 mM ethanolic solution of HS(CH12)15COOH

(dit is mercaptohexadecanoic acid, in kast op 11de

Immerse into aqueous equal volume mixture of

400 mM carbodiimide EDC (in vriezer 702)

100 mM NHS (in koelkast 702)

for 1 hour

Rinse in ultrapure water and dry

Place into solution of protein

(Rachel: 23 mg/ml shikimate kinase, pH 4.9 for

time 0,10,30,60,120 mins-24 hrs monitor coverage)

From: McKendry et al., Nature 391, 566-568 (1998)

Figure: