Nanotube tip shortening

set-up

- cover the piezo with a piece of plastic (double parafilm)

- on top of this comes the voltage pulse wire (black and white)

- on top of this a metal puck with a Si surface attached to it with silver paint

If you do these three steps the evening before you want to do the shortening, the plastic has time to equilibrate

- the tip is grounded by putting a grounding wire (brown) between the tip holder and one of the two screws that fasten the tip holder

- do not yet connect the high voltage output to the puck!

lab view

open VI \ user.lib \ tjerk \ tip shortening program

pulse train: this gives a trigger to the card

pulser 2 amplify by 20: gives high voltage outputs between -40 and 40 V, with a pulse length of 100 microseconds and reads the z-voltage of the piezo

start with pulses of 2 V, do not go higher than 20 V

- to activate a program, swith it on and press RUN (white arrow)

- to give a pulse, press GO

- it is better to stop the lab view programs before starting the nanoscope program, otherwise it will operate very slowly

high voltage amplifier

- the IN cable of the card goes to the bias box LV Z output

the OUT cable of the card must be connected to the input of the high voltage 	amplifier

- first check the output of the high voltage amplifier (monitor output) on an oscilloscope (DC, 10 mV, 50 microseconds)

- now you can connect the high voltage output to the puck

AFM

- the AFM is operated in Tapping Mode

- scan area: 500 nm x 500 nm

- give a pulse during scanning and check if the z piezo voltage increases (which means that you have reduced the length of the nanotube)