# Preparation of lipid bilayers – with freeze/thaw

 Dissolve lipids in chloroform (for example: 1mg) in a glass beaker

 Evaporate the chloroform under a stream of nitrogen

 Resuspend the lipids in 20mM NaCl (or other aqueous buffer; to a concentration of for example 1 mg/ml or 10mM. You should have at least 2 ml ). Leave for ca ½ hour to proprely dilute.

 Make sure the plug is well fixed in your bottle!  Freeze/thaw by holding the bottel first in liquid nitrogen and then carefully melt in hot water. Make sure it is properly frozen by hearing/seeing cracks  and stop heating as soon as you see it melt.  Repeat 5-10 times.

 Transfer to small, wide necked bottles for sonnication.

 Sonication: The temperature of the solution will increase during sonication, so keep the glass bottle in ice, while sonicating.The microtip should be well immersed in your solution, but NOT touch the glass. Sonicate the solution with the microtip sonicator for at least 30 min [duty on (50%), level at 4].  Remember to tune the sonicator before you start and to check the tuning after a few minutes of sonnicating.

You should end up with a transparent solution.

 During sonication you will get bits of metal from the tip in your solution, so next step is transfer to eppendorfs for spinning and discarding the pellet.

Your vesicles are ready

 Adsorb a droplet (75ul) of the solution on freshly cleaved mica. Incubate 15-30 minutes. Rinse by exhanging buffer 5-10 times

 Image in your buffer

author: Henriette Jensenius, June 2004